To make the use of x-ray inspection easier to interpret during inspection or after rework a teardrop pad is used to connect to the track. This allows the solder ball and solder paste to wet away from the pad during reflow.

The solder joints viewed after reflow show a solder nipple projecting from the joint area. This makes inspection a simpler task.

For further information on BGA Technology contact the Engineering Department of Osborne Electronic. Training videos on BGA Technology, Rework and Repair of BGA and X-Ray Inspection of BGA are available in the industry and Osborne Electronics have further information on their availability.

ãBob Willis Electronic Presentations Services

Bob Willis BGA (Ball Grid Array) Design Rules

The following design rules are provided by EPS and may be used for BGA (Ball Grid Array) component s. These basic design rules along with other design requirements will assist our customers  produce a reliable product.

All BGA pads should be the same size between 0.020-0.025” with track connection between 0.008-0.010”.

The solder resist aperture layer is produced between 0.004-0.006” larger than the BGA pad to give normal clearance for PCB manufacture using photo imagable solder resist.

Corner marks are required on a minimum of two opposite sides of each BGA component to aid inspection after placement, manual assembly and to allow replacement after rework.. Typically the mark widths will be 0.010-0.015” positioned half under the edge of the BGA outline.

The marks should ideally be etched into the copper layer as this will provide the most accurate alignment with the BGA pad pattern. The use of legend marks should be avoided as they are not as accurate and this provides the opportunity to eliminate legend from the board design and save cost.